## Slide 1
Supporting Information C (SI_C) to

## Slide 2: LDIR Analysis

## Slide 3
All samples were transferred onto Ag-coated slides
Laser direct infrared (LDIR) Imaging

## Slide 4
Automated laser direct infrared imaging (20 – 500 µm; HQI : 85%)
Leachate samples for particle analysis
(200 µL of the leachates)
Laser direct infrared (LDIR) Imaging

## Slide 5
Highlights
PE 2 and PET 1  High numbers of microplastics (particles and fibers) were generated/released:
PE 2 (one PE and one PET side) : ~ 400 (dark control) and ~ 3280 (UV treated) fibers mL-1  UV-induced effects seem to be dominant
PET 1: ~ 2460 (dark control) and ~ 2810 SAN (UV treated) particles mL-1  Mechanical effects seem to be dominant

## Slide 6: Blank_1_DC
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 13 | 3 | 0 | 0 | 0 | 16 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 13 | 3 | 0 | 0 | 0 | 16 | 
Sum MPs | 0 | 0 | 0 | 0 | 0 | 0 | 
Particles < 100 | 16 |  |  |  |  |  | 
MPs < 100 | 0 |  |  |  |  |  | 
200 µL

## Slide 7: Blank_1_UV
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 5 | 3 | 0 | 0 | 0 | 8 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 5 | 3 | 0 | 0 | 0 | 8 | 
Sum MPs | 0 | 0 | 0 | 0 | 0 | 0 | 
Particles < 100 | 8 |  |  |  |  |  | 
MPs < 100 | 0 |  |  |  |  |  | 
200 µL

## Slide 8: Blank_2_DC
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 5 | 0 | 0 | 0 | 0 | 5 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 5 | 0 | 0 | 0 | 0 | 5 | 
Sum MPs | 0 | 0 | 0 | 0 | 0 | 0 | 
Particles < 100 | 5 |  |  |  |  | 5 | 
MPs < 100 | 0 |  |  |  |  |  | 

## Slide 9: Blank_2_UV
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 7 | 0 | 0 | 0 | 0 | 7 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 5 | 1 | 0 | 0 | 0 | 6 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 2 | 0 | 0 | 0 | 0 | 2 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 14 | 1 | 0 | 0 | 0 | 15 | 
Sum MPs | 7 | 1 | 0 | 0 | 0 | 8 | 
Particles < 100 | 15 |  |  |  |  | 7 | 
MPs < 100 | 8 |  |  |  |  |  | 
100 µL

## Slide 10: PVC_1_DC
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 119 | 7 | 1 | 1 | 0 | 128 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 2 | 0 | 0 | 0 | 0 | 2 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 3 | 1 | 1 | 0 | 0 | 5 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 124 | 8 | 2 | 1 | 0 | 135 | 
Sum MPs | 5 | 1 | 1 | 0 | 0 | 7 | 
Particles < 100 | 132 |  |  |  |  |  | 
MPs < 100 | 6 |  |  |  |  |  | 
200 µL

## Slide 11: PVC_1_UV
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 24 | 4 | 0 | 0 | 0 | 28 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 3 | 2 | 0 | 0 | 0 | 5 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 1 | 0 | 0 | 0 | 0 | 1 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 28 | 6 | 0 | 0 | 0 | 34 | 
Sum MPs | 4 | 2 | 0 | 0 | 0 | 6 | 
Particles < 100 | 34 |  |  |  |  | 28 | 
MPs < 100 | 6 |  |  |  |  |  | 
200 µL

## Slide 12: PVC_2_DC
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 33 | 1 | 0 | 0 | 0 | 34 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 33 | 1 | 0 | 0 | 0 | 34 | 
Sum MPs | 0 | 0 | 0 | 0 | 0 | 0 | 
Particles < 100 | 34 |  |  |  |  |  | 
MPs < 100 | 0 |  |  |  |  |  | 
200 µL

## Slide 13: PVC_2_UV
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 32 | 1 | 0 | 0 | 0 | 33 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 2 | 1 | 0 | 0 | 0 | 3 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 1 | 0 | 0 | 0 | 1 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 34 | 3 | 0 | 0 | 0 | 37 | 
Sum MPs | 2 | 2 | 0 | 0 | 0 | 4 | 
Particles < 100 | 37 |  |  |  |  |  | 
MPs < 100 | 4 |  |  |  |  |  | 
200 µL

## Slide 14: PET_1_DC
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 49 | 3 | 1 | 0 | 0 | 53 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 1 | 0 | 0 | 0 | 0 | 1 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS (SAN !) | 194 | 38 | 13 | 1 | 0 | 246 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 244 | 41 | 14 | 1 | 0 | 300 | 
Sum MPs | 195 | 38 | 13 | 1 | 0 | 247 | 
Particles < 100 | 285 |  |  |  |  | 53 | 
MPs < 100 | 233 |  |  |  |  |  | 

## Slide 15: PET_1_DC
100 µL

## Slide 16: PET_1_DC
100 µL

## Slide 17: PET_1_UV
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 359 | 50 | 10 | 7 | 0 | 426 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 1 | 0 | 0 | 0 | 0 | 1 | 0
PVC | 49 | 2 | 1 | 0 | 0 | 52 | 0
PA | 52 | 1 | 0 | 0 | 0 | 53 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 1 | 0 | 0 | 0 | 0 | 1 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS (SAN !) | 240 | 33 | 8 | 0 | 0 | 281 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 73 | 6 | 0 | 1 | 0 | 80 | 0
total | 775 | 92 | 19 | 8 | 0 | 894 | 
Sum MPs | 416 | 42 | 9 | 1 | 0 | 468 | 
Particles < 100 | 867 |  |  |  |  |  | 
MPs < 100 | 458 |  |  |  |  |  | 

## Slide 18: PET_1_UV
100 µL

## Slide 19: PET_1_UV
100 µL

## Slide 20: PET_1_UV
100 µL

## Slide 21: PET_1_UV
100 µL

## Slide 22: PET_1_UV
100 µL

## Slide 23: PET_1_UV
100 µL

## Slide 24: PET_2_DC
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 114 | 7 | 1 | 0 | 0 | 122 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 1 | 1 | 0 | 0 | 0 | 2 | 0
Acrylates/PU/Varnish | 157 | 28 | 0 | 0 | 0 | 185 | 0
PVC | 23 | 3 | 0 | 0 | 0 | 26 | 0
PA | 4 | 0 | 0 | 0 | 0 | 4 | 0
EVA | 1 | 0 | 0 | 0 | 0 | 1 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 668 | 47 | 9 | 0 | 0 | 724 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 185 | 7 | 1 | 0 | 0 | 193 | 0
PS | 4 | 0 | 0 | 0 | 0 | 4 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 3 | 0 | 0 | 0 | 0 | 3 | 0
PET | 27 | 0 | 0 | 0 | 0 | 27 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 1187 | 93 | 11 | 0 | 0 | 1291 | 
Sum MPs | 1073 | 86 | 10 | 0 | 0 | 1169 | 
Particles < 100 | 1280 |  |  |  |  |  | 
MPs < 100 | 1159 |  |  |  |  |  | 

## Slide 25: PET_2_DC
100 µL
Interfering precipitate

## Slide 26: PET_2_DC
100 µL

## Slide 27: PET_2_UV
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 131 | 1 | 0 | 0 | 0 | 132 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 1 | 0 | 0 | 0 | 0 | 1 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 3 | 0 | 0 | 0 | 0 | 3 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 1 | 0 | 0 | 0 | 0 | 1 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 136 | 1 | 0 | 0 | 0 | 137 | 
Sum MPs | 5 | 0 | 0 | 0 | 0 | 5 | 
Particles < 100 | 137 |  |  |  |  |  | 
MPs < 100 | 5 |  |  |  |  |  | 

## Slide 28: PET_2_UV
100 µL
Interfering precipitate

## Slide 29: PE_1_DC
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 27 | 3 | 1 | 0 | 0 | 31 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 1 | 0 | 0 | 0 | 0 | 1 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 28 | 3 | 1 | 0 | 0 | 32 | 
Sum MPs | 1 | 0 | 0 | 0 | 0 | 6 | 
Particles < 100 | 31 |  |  |  |  |  | 
MPs < 100 | 1 |  |  |  |  |  | 
200 µL

## Slide 30: PE_1_UV
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 16 | 5 | 0 | 0 | 0 | 21 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 16 | 5 | 0 | 0 | 0 | 21 | 
Sum MPs | 0 | 0 | 0 | 0 | 0 | 0 | 
Particles < 100 | 21 |  |  |  |  |  | 
MPs < 100 | 0 |  |  |  |  |  | 
200 µL

## Slide 31: PE_2_DC
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 5 | 0 | 1 | 0 | 0 | 6 | 0
PE | 1 | 1 | 0 | 0 | 0 | 2 | 0
PP | 1 | 0 | 0 | 0 | 0 | 1 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 6 | 22 | 11 | 1 | 0 | 40 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 13 | 23 | 12 | 1 | 0 | 49 | 
Sum MPs | 8 | 23 | 11 | 1 | 0 | 43 | 
Particles < 100 | 36 |  |  |  |  | 6 | 
MPs < 100 | 31 |  |  |  |  |  | 

## Slide 32: PE_2_DC
100 µL

## Slide 33: PE_2_DC
100 µL

## Slide 34: PE_2_UV
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 54 | 4 | 2 | 0 | 0 | 60 | 0
PE | 1 | 0 | 0 | 0 | 0 | 1 | 0
PP | 2 | 0 | 0 | 0 | 0 | 2 | 0
Acrylates/PU/Varnish | 0 | 1 | 0 | 0 | 0 | 1 | 0
PVC | 0 | 1 | 0 | 0 | 0 | 1 | 0
PA | 11 | 0 | 0 | 0 | 0 | 11 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 153 | 98 | 62 | 14 | 1 | 328 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 221 | 104 | 64 | 14 | 1 | 404 | 
Sum MPs | 167 | 100 | 62 | 14 | 1 | 344 | 
Particles < 100 | 325 |  |  |  |  | 60 | 
MPs < 100 | 267 |  |  |  |  |  | 
100 µL

## Slide 35: PE_2_UV
100 µL

## Slide 36: PE_2_UV
100 µL

## Slide 37: PE_2_UV
100 µL

## Slide 38: PE_3_DC
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 2 | 0 | 0 | 0 | 0 | 2 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 1 | 0 | 0 | 0 | 0 | 1 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 1 | 0 | 0 | 0 | 1 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 3 | 1 | 0 | 0 | 0 | 4 | 
Sum MPs | 1 | 1 | 0 | 0 | 0 | 2 | 
Particles < 100 | 4 |  |  |  |  |  | 
MPs < 100 | 2 |  |  |  |  |  | 

## Slide 39: PE_3_UV
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 6 | 1 | 0 | 0 | 0 | 7 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 1 | 0 | 0 | 0 | 0 | 1 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 0 | 0 | 0 | 0 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 7 | 1 | 0 | 0 | 0 | 8 | 
Sum MPs | 1 | 0 | 0 | 0 | 0 | 1 | 
Particles < 100 | 8 |  |  |  |  |  | 
MPs < 100 | 1 |  |  |  |  |  | 

## Slide 40: PE_4_DC
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 16 | 1 | 0 | 0 | 0 | 17 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylates/PU/Varnish | 5 | 0 | 0 | 0 | 0 | 5 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 2 | 0 | 0 | 0 | 0 | 2 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 1 | 2 | 0 | 0 | 0 | 3 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 24 | 3 | 0 | 0 | 0 | 27 | 
Sum MPs | 8 | 2 | 0 | 0 | 0 | 10 | 
Particles < 100 | 27 |  |  |  |  |  | 
MPs < 100 | 10 |  |  |  |  |  | 

## Slide 41: PE_4_UV
100 µL
Type Cluster d [µm] | 20-50 | 50 - 100 | 100 - 200 | 200 - 500 | > 500 | Sum | Control
Natural components | 31 | 5 | 3 | 0 | 0 | 39 | 0
PE | 0 | 0 | 0 | 0 | 0 | 0 | 0
PP | 1 | 0 | 0 | 0 | 0 | 1 | 0
Acrylates/PU/Varnish | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PA | 0 | 0 | 1 | 0 | 0 | 1 | 0
EVA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PC | 0 | 0 | 0 | 0 | 0 | 0 | 0
PTFE | 0 | 0 | 0 | 0 | 0 | 0 | 0
Rubber | 0 | 0 | 0 | 0 | 0 | 0 | 0
PLA | 0 | 0 | 0 | 0 | 0 | 0 | 0
PE-Cl | 0 | 0 | 0 | 0 | 0 | 0 | 0
PS | 0 | 0 | 0 | 0 | 0 | 0 | 0
PMMA | 0 | 0 | 0 | 0 | 0 | 0 | 0
Acrylonitile butadiene | 0 | 0 | 0 | 0 | 0 | 0 | 0
Silicone | 0 | 0 | 0 | 0 | 0 | 0 | 0
PET | 0 | 0 | 0 | 0 | 0 | 0 | 0
Unknown | 0 | 0 | 0 | 0 | 0 | 0 | 0
PVDC | 0 | 0 | 0 | 0 | 0 | 0 | 0
total | 32 | 5 | 4 | 0 | 0 | 41 | 
Sum MPs | 1 | 0 | 1 | 0 | 0 | 2 | 
Particles < 100 | 37 |  |  |  |  |  | 
MPs < 100 | 1 |  |  |  |  |  |