## Slide 1
Supporting Information D (SI_D) to

## Slide 2: Workflow and instrument described in detail in Hildebrandt et al. (2021; HAZMAT) https://www.sciencedirect.com/science/article/pii/S0304389421004453
ATR-FTIR analysis

## Slide 3
Analysis of raw materials

## Slide 4
PVC 1

## Slide 5
PVC 2

## Slide 6
PE 1

## Slide 7
PE 2
One side is PET and one side is PE

## Slide 8
PE 3
Polyethylene (89.2% agreement)

## Slide 9
PE 4

## Slide 10
PE 4
Polyethylene (91.4% agreement)
Black and white side show very similar spectra

## Slide 11
PET 1
PET 1 consisted of 2 parts which are of the same material

## Slide 12
PET 1
 Styrene acrylonitrile copolymer (SAN) (75% agreement), visually good agreement (2 different reference spectra are shown in blue and pink)
C≡N / nitrile functional group  not PET !

## Slide 13
PET 2 – glass fiber reinforced polyester

## Slide 14
PET 2
Database comparison of original spectra (70.4% agreement with cellulosic, but the spectra look different)
 No good/suitable assignment, composite material ?

## Slide 15
PET 2
Visual comparison of PET (red) and Housing spectrum
 No good/suitable assignment, composite material ?

## Slide 16
Analysis of dark control and UV treated plastic pieces

## Slide 17
ATR-FTIR analysis to study carbonyl index and OH bands as indicators of oxidation
Spectral comparison with the raw materials and between UV-treated and dark controls

## Slide 18
PE 1 and 3
UV-raw comparison
 No significant changes/oxidation

## Slide 19
UV-raw comparison
 Increase of the carbonyl band, indication of significant UV weathering
2 layer material: one PET and one PE side !
PE side
PE 2

## Slide 20
UV-raw comparison
 No significant changes/oxidation
PET side
2 layer material: one PET and one PE side !
PE 2

## Slide 21
One white and one black side with similar IR spectra
UV-raw comparison
 No significant changes/oxidation
Black side
PE 4

## Slide 22
No significant differences between DC, UV and raw material spectra
No signs of oxidation (carbonyl band)
PVC 1 DC  930/1000 agreement with raw spectrum PVC 1 UV  896/1000 agreement with raw spectrum
14
PVC 1

## Slide 23
16
Very thin grey layer !
PVC 1

## Slide 24
No significant differences between DC, UV and raw material spectra
No signs of oxidation (carbonyl band)
PVC 2 DC  943/1000 agreement with raw spectrum PVC 2 UV  951/1000 agreement with raw spectrum
15
PVC 2

## Slide 25
Not PET but SAN
UV-raw comparison
DC-raw comparison
Differences between the dark control (DC) and UV spectra; increase of the carbonyl and OH band in the spectrum of the UV-treated material
PET 1

## Slide 26
Unknown, glass fiber reinforced polyester
 No significant differences
DC-UV comparison
PET 2